## Slide 1: General manufacturing process and Energy Conservation opportunities in Handtool Cluster
By Er. Gurinder Jeet Singh

## Slide 2: ABOUT DELTA ENERGY NATURE
DELTA ENERGY NATURE WAS ESTABLISHED IN 1999 TO PROVIDE TECHNICAL SUPPORT FOR REHEATING PROCESS .
AT THAT TIME REHEATING PROCESS IN INDIA WERE VERY MUCH RUDE .
PEOPLES WERE THINKING IF THEY WILL DELIVER MORE OIL TO FURNACE MATERIAL WILL HEAT MORE . THEY WERE NOT TAKING CARE FOR BLACK SMOKE EVOLVING FROM FURNACE .

## Slide 3
WE PROVIDED TEMPRATURE CONTROL SYSTEM TO REHEATING FURNACES . THIS SYSTEM WAS CAPABLE TO CONTROL THE FURNACE WITH IN ±3°C .
WITH THIS SYSTEM HUMAN INTERVENTION BECOME MINIMUM .
WITH THE HELP OF THIS SYSTEM WE FIXED OIL AND AIR FLOW . IT HELPED TO ACHIEVE MAX ELEVATED TEMP .

## Slide 4
FEW FIREMAN AND FOREMAN OBJECTED THAT THEY NEED MORE OIL TO HEAT UP FURNACE AND MATERIAL .
I ALLOWED THEM TO INCRESE OIL . WHEN THEY INCREASED OIL BLACK SMOKE START EVOLVE . BECAUSE OF CARBON MONO OXIDE FORMATION START.
TEMPRATURE CONTROLER WAS TELLING TEMPRATURE IN FURNACE IS FALLING . WITH IN 3 MIN 34°C FALL IN TEMP . PRACTICALLY PROVED.

## Slide 5: WELCOME TO FRIENDS FROM NAGUR
LUCKLY I VISITED YOUR PLACE AND HAD OBSERVATION FOR ONE DAY .
YOU PEOPLES ARE UNIQUE . YOU ARE WORKING WITH LEAST RESOURCES AND ARE BEST EFFICIENT.
BEING FAMILY RUN UNITS YOU ARE HIGHLY PRODUCTIVE , YOU GOT +VE ATTITUDE & YOUR JACKARDS ARE EXCELLENT . Especially forging M/C
I SALUTE YOU FOR YOUR WAY OF WORKING AND COMPETTING LOW END SEGENT .

## Slide 6
I DID NOT OFFERED YOU FURNACE SINCE LAST 3 YEARS . THERE ARE FEW REASONS AS BELOW .
YOU DO FORGING FOR ONLY 8 HRS A DAY . FORGING IS HOT OPERATION YOU SHOULD RUN YOUR FORGING MACHINES 24 HRS . 24X6 MINIMUM . ONLY THEN I CAN GIVE YOU FURNACE
YOU ARE NOT QUALITY CONCIOUS . FEW PEOPLE ARE USING PROPER GRADED RAW MATERIAL . OTHERS ARE USING OLD MILD STEEL SARIYA USED SCRAPE FROM OLD ROOFS .

## Slide 7
UPTO CERTAIN LEVEL PEOPLES CAN DO AS YOU ARE DOING . FOR YOUR PRODUCT YOU ARE GETTING LESS PRICE .
IF YOU MANUFACTURE GOOD QUALITY PRODUCT . YOU CAN ASK FOR BETTER PRICE .
WHEN PRODUCTION OF A UNIT CROSSES A CERTAIN LEVEL THEN ONLY SYSTEM RUN THE COMPANY AND PRODUCE CONSISTANENT QUALITY PRODUCT .

## Slide 8
video 1
Video 2
Video 3
Video 4
Video 5

## Slide 9: General manufacturing practices
HAND TOOL MANUFACTURING START WITH BLANK CUTTING .
BEFORE THIS MATERIAL SHOULD BE CERTIFIED FROM QUALITY CONTROL DEPARTMENT .
IT SHOULD NOT HAVE CRACKS .
REFRACTORY INCLUSION IN MATERIAL SHOULD BE WITH IN TOLERANCE .
SHULPER & PHOSE SHOULD NOT EXCEED 0.04%

## Slide 10
WHEN WE SELECT A PROPER MATERIAL ONLY THEN WE CAN MANUFACTUR GOOD QUALITY END PRODUCT .
FOR BLANK CUTTING MACHINE EXACT SIZE ELECTRIC MOTOR SHOULD BE USED.
IF WE USE BIG MOTOR IT WILL DRAG POWERFACTOR TO LOWER SIDE & CREATE IN EFFICIENCY ON ELECTRICAL SIDE .
IF WE USE STEEL ROD INSTEAD OF PROFILE STRENGTH OF FINISHED MATERIAL IS MORE BY 25%

## Slide 11
FORGING OPERATION COMPOSE OF REHEATING FURNACE POWER HAMMER AND DIE MOULD . THIS PROCESS CALLED CLOSE DIE FORGING .
ALMOST 60% ENERGY IS CONSUMED AT THIS PROCESS . SO SCOPE OF CONSERVATION IS MORE .
A LOT OF TIME WE ARE CREATING IN EFFICIENCY BECAUSE OF IGNORANCE . IF WE TAKE OUT 2 PCS FOR FORGING 2ND PC WILL GET HOLD FOR 5-6 SEC IT WILL LOSE ITS ORIGNAL TEMP. BAD HABIT.

## Slide 12
SOME TIME WORKER TAKE OUT 3 PCS ONCE . FOR 3RD PIECE WE ARE TO HOLD IT FOR 10-12 SEC. IT COOL DOWN BELOW800°C . WHEN THIS PIECE IS FORGED , CAVITY IN DIE DAMGES
AIR JETS WHICH ARE USED TO REMOVE SLAG FROM DIE ARE NOT HAVING GOOD SHAPE NOZEL . A PART OF AIR FROM THIS JET DIVERT AND HIT HOT MATERIAL IN TURN AT ANVIL. EVIDENCE OF THIS IS A PORTION OF BLANK IS HOT AND OTHER IS COLD. SO KEEP CARE OF AIR JETS .

## Slide 13
FOCUS OF AIR JET IS NOT CORRECT . A PART OF AIR IS HITTING HOT MATERIAL IN TURN . IT IS ALSO CAUSING HOT COLD SPOT AT SAME BALNK . CONSEQUENCES YOU KNOW BETTER.
RATE OF PRODUCTION SHOULD BE CONSISTANT WITH IN ±10% . IT IS OBSERVED WHEN WORKER START WORK STARTING HOURS HIS ENERGY LEVEL IS MORE HE TAKE OUT 850 PC AVG FOR 1ST 3 HOURS . THEN LAST HOURS OF SHIFT. HIS PRODUCTION RATE FALL TO 500 PCS AVG . THIS TYPE OF PATTREN OF PRODUCTION REDUCES EFFICIENCY OF FURNACE.

## Slide 14
IN FEW COMPANIES THEY FEED MAREIAL FROM EXIT DOOR AS BATCH TYPE OPERATION BY DOING THIS PRACTICE MATERIAL WHICH ENTER THE FURNACE DIP INSIDE THE HEAP OF MATERIAL AFTER 10 MIN WHEN TEMP BECOME UNIFORN THEY START TAKE OUT MATERIAL . MATERIAL WHICH WAS FED LAST IS BEING TAKEN OUT 1ST . AND MATERIAL WHICH WAS FED 1ST TAKEN OUT LAST . HEATING TIME FOR 1ST FED PC IS 20 MIN AND HEATING TIME FOR LAST FED PC IS 10 MIN.
AVIOD THIS PRACTICE AND APPLY FIFO

## Slide 15
TRIMING IS DONE ON TRIMMING PRESS WITH THE HELP OF DEDICATED DIE PUNCH .
MATERIAL IS CLEANED IN SHOT BLASTING MACHINE .
IT IS DEBURRING ON VIBRATOR MACHINE .
IF SURFACE OF FORGED MATERIAL IS HAVING PITTING OR DENT MARKS THEN MATERIAL IS GRINDED WITH THE HELP OF BELT GRINDER OR AUTOMATIC MACHINES .

## Slide 16
WITH PROPER FINISH AT SURFACE MATERIAL IS BEING ELECTRO PLATING .
LAYER OF NICKEL AND CHROME IS BEING DEPOSIT ON STEEL SURFACE AS PER CUSTOMER REQUIREMENT .
AS PER OUR SURVEY ENERGY USED TO CREATE STEAM FOR NICKEL PLANT CAN BE SAVED AND ENVIORNMENT IN THIS AREA WILL ALSO IMPROVE WE ARE WORKING ON THIS AND WILL PROVIDE SOLUTION FOR THIS AREA .

## Slide 17
FINAL INSPECTION IS DONE AND
PACKING IS MADE AS PER CUSTOMER REQUIREMENT .
THIS IS THE COMPLETE PROCESS ADOPTED IN HAND TOOL FACTORY .

## Slide 18
THANKING YOU .